## Slide 1
Polymer Electrolyte | σRT (S/cm)
Celgard+Na2SiON | 1.0 ± 0.8 x 10-6
Celgard+Na4SiON | 1.1 ± 0.5 x 10-6

## Slide 2
NaxSiPON (x = Na/P) Precursors
NaxSiON (x = Na/Si) Precursors

## Slide 4
Stainless Steel (SS)/NaxSiON PE/SS
SEM Fracture Surfaces of Na3SiPON coated NAMO